## Slide 1: Lecture schedule October 3 – 7, 2011
#1 Kondo effect
#2 Spin glasses
#3 Giant magnetoresistance
#4 Magnetoelectrics and multiferroics
#5 High temperature superconductivity
#6 Applications of superconductivity
#7 Heavy fermions
#8 Hidden order in URu2Si2
#9 Modern experimental methods in correlated electron systems
#10 Quantum phase transitions
Present basic experimental phenomena of the above topics
Present basic experimental phenomena of the above topics
Heavy Fermions

## Slide 2: Heavy Fermions: Experimentally discovered -- CeAl3 (1975), CeCu2Si2 (1979) and Ce(Cu6-x Aux) (1994) At present not fully explained theoretically
Large effective mass - m*
Loss of local moment magnetism
Large electron-electron scattering
Renormalized heavy Fermi liquid
Unconventional superconductivity from heavy mass of f-electrons
Other unusual ground state properties appearing out of heavy Fermi liquid, e.g., reduced moment antiferromagnetism, hidden order; quantum phase transitions.
Various phenomenological theories and models.
Example of strongly correlated electrons systems (SCES).

## Slide 3: What are SCES: An experimentalist’s sketch
H = KE + {U,V,J,Δ}, Bandwidth (W) vs interactions
e.g., H = ∑ t ij c†i,σ cj,σ + U ∑ ni↑ n i↓ Hubbard Model
If {U,V,J,Δ} >> W, then SCES, e.g. Mott-Hubbard insulator.
See sketch. What type of systems ? TM oxides.
H = KE + HK + HJ , Bandwidth (W) vs interactions
e.g., H = ∑ εk c†k ck + JK∑Sr·(c†σc) + JH∑ Sr · Sr’
Kondo/Anderson Lattice Model
If {JK,J} >> εk (W), then SCES, e.g. HFLiq, NFL, QCPt.
See sketches. What type of systems ? 4f &5f intermetallics.

## Slide 5: Metallic systems: Temperature vs JH. Unconventional Fermi liquids to local moment (antiferro)magnetism.
J
Senthil, S. Sachdev & M. Vojta, Physica B 359-361,9(2005)

## Slide 6: Metallic systems: Temperatute vs JK. Unconventional Fermi liquid to Kondo state - conventional FL.
Novel U(1)FL* fractionalized FL with deconfined neutral S=1/2 excitations. U(1) is the spin liquid gauge group. <b> (slave boson) measures mixing between local moments and conduction electrons.
Theoretical Proposal from T. Senthil et al. PRB (2004).

## Slide 7
Generic magnetic phase diagram resulting from HFLiq.
tunable ground state properties  control parameter d
unconventional superconductivity/novel phases
quantum critical behavior (Non-Fermi-Liquid)
SC
ultra-low moment magnetism / “Hidden Order“
d
experimental:
pressure
d
magnetic hybrid. strength J
d
experimental:
mag. field
pressure
substitution

## Slide 8: How to create a heavy fermion? Review of single-ion Kondo effect in T – H space. (Note single impurity Kondo state is a Fermi liquid!)
Crossover in H & T

## Slide 9: Now the Kondo lattice DOS with FS volume increased
Possibility of real phase transitions
“Kondo insulator” small energy gap in DOS at EF

## Slide 10: Cartoon of Doniach phase diagram (1976): Kondo vs RKKY on lattice

## Slide 11: Doniach phase diagram can be pressure tuned
U-based compounds ???

## Slide 12: Instead of single impurity Anderson or Kondo models, need periodic Anderson model (PAM) – not yet fully solved
Note summation over lattice sites: i and j

## Slide 13: Extension of our old friend the single imputity Anderson model to the Anderson/Kondo lattice. Now PAM
Nice to have Hamiltonian but how to solve it? Need variety of interactions: c-c, c-f; f-f which are non-local, i.e., itinerant – band structure.

## Slide 14: Elements with which to work and create HFLiq.
Mostly METALS, almost all under pressure superconducting ! Consider SCES that are intermetallic compounds, “Heavy Fermions”.

## Slide 16: Basic properties of HF’s. For an early summary, see G.R. Steward, RMP 56(1984), 755.
Specific heat and susceptibility (as thermodynamic properties), and resistivity and thermopower (as transport properties) with m* as renormalized effective mass due to large increase in density of states at EF.
T* represents a crossover “coherence” temperature where the magnetic local moments become hybridized with the conduction electrons thereby forming the heavy Fermi liquid. (Sometimes called the Kondo lattice temperature).
Key question here is what forms in the ground state T  0: a vegetable (heavy spin liquid), e.g. CeAl3 or CeCu6, or something more interesting.
What is the mechanism for the formation of heavy Fermi liquid: Kondo effect with high T quenching of Ce, Yb; U moments or strong hybridization of these moments with the itinerant conduction electrons?

## Slide 17: CV/T vs T showing the spin entropy for UBe13. Note the dramatic superconducting transition at TC = 0.9K and the large γ-value (1 J/mole-K2) for T>TC
Fall-off of C/T into superconducting state – power laws: nodes in SC gap

## Slide 18: Susceptibility – enhanced yet constant at lowest temperatures, problems with residual impurities. Not Curie-Weiss-like!
  constant as T  0 (enhanced Pauli-very large DOS at EF) but band structure effects intervene at low temperatures creating maxima.

## Slide 19: More susceptibility: CeCu6 (HFLiq) and UPt3 (HF-SC, TC = 0.5K). Note ad-hoc fit attempts of (T)

## Slide 20: Collection of resistivity vs T data for various HF’s
Note large ρ(T) at hiT[large spin fluc./Kondo scattering] and lowT ρ(T) = ρo + AT2 [heavy Fermi liquid state with large A-coefficient.]

## Slide 21: Relations between the three experimental parameters γ, χ, and ρ in HFLiq. State: Wilson ratio
Wilson ratio of low T susceptibility to specific heat coefficient.
Directly follows from Fermi liquid theory with large m*

## Slide 22: Kadowaki – Woods ratio: γ2/A = const(N). Complete collection of HF materials. Note slope = 2 in log/log plot
Recent theory can account for different N-values

## Slide 23: Extended Drude model for heavy fermions to analyze optical conductivity measurements
σ(ω) = ωp/[4π(τ-1 – iω)] where σ = σ1 + iσ2
ωp = 4πne2/m
σ1 = ωpτ-1/[4π(τ-2 + ω2)]
σ2 = ωp2ω/[4π(τ-2 + ω2)]
1/τ(ω) = ωσ1(ω)/σ2(ω) = [ωp(ω)/4π]Re[1/σ(ω)]
1/ωp2(ω) = [1/4πω]Im[-1/σ(ω)]
For mass enhancement: m*/m = 1 + λ
τ(ω) = (m*/m)τo(ω) = [1 + λ(ω)]τo(ω) and ωp2(ω) = ωp2/[1 + λ]
1 + λ(ω) = [ωpo2/4πω]Im[-1/σ(ω)
Fermi liquid theory: 1/τo(ω) = a (ħω/2π)2 + b(kBT)2
where b ≈ 4 old Fermi liquid theory and b ≈ 1 for some new heavy fermions

## Slide 24: Optical conductivity σ(ω) of generic heavy fermion: T > T* and T < T* formation of hybridization gap, i.e., a partial gapping usually called pseudo gap.
T < T*: large Drude peak
T > T*
Hybridization gap
Note shifting of spectral weight from pseudo gap to large Drude peak
σ(ω) = (ne2/m*) [τ*/(1 + ω2τ*2]
1/τ* = m/(m*τ) renormalized effective mass & relaxation rate

## Slide 25: New physics with disorder: The magnetic phase diagram of heavy fermions (phenomenologically). Pressure vs disorder and non Fermi liquids (NFL).
inequivalent
control parameters
pressure = J
≠
disorder = J
disorder and NFL behavior?
substitutional disorder?
chem. pressure
substitution

## Slide 26: Non Fermi liquid behavior: What is it ??? Previously used term “quantum critical” in vicinity (above) of QCP
HFLiq.renormal-ized by m*:  = o + AT2
Deviations from above FL behavior
NFL →
More in #10 Quantum Phase Transitions

## Slide 27: STOP

## Slide 28
New physics: the magnetic phase diagram of heavy fermions (phenomenologically)
inequivalent
control parameters
pressure = J
≠
disorder = J
disorder and NFL behavior?
substitutional disorder?
chem. pressure
substitution

## Slide 29
Generic magnetic phase diagram
tunable ground state properties  control parameter d
unconventional superconductivity/novel phases
quantum critical behavior (Non-Fermi-Liquid)
SC
ultra-low moment magnetism / “Hidden Order“
d
experimental:
pressure
d
magnetic hybrid. strength J
d
experimental:
mag. field
pressure
substitution

## Slide 31: Lecture schedule October 3 – 7, 2011
#1 Kondo effect
#2 Spin glasses
#3 Giant magnetoresistance
#4 Magnetoelectrics and multiferroics
#5 High temperature superconductivity
#6 Applications of superconductivity
#7 Heavy fermions
#8 Hidden order in URu2Si2
#9 Modern experimental methods in correlated electron systems
#10 Quantum phase transitions
Present basic experimental phenomena of the above topics
Present basic experimental phenomena of the above topics

## Slide 32: Elements with which to work

## Slide 33: What are SCES ?
H = KE + {U,V,J,Δ}, Bandwidth (W) vs interactions
e.g., H = ∑ t ij c†i,σ cj,σ + U ∑ ni↑ n i↓ Hubbard Model
If {U,V,J,Δ} >> W, then SCES, e.g. Mott-Hubbard insulator.
See sketch. What type of systems ? TM oxides.
H = KE + HK + HJ , Bandwidth (W) vs interactions
e.g., H = ∑ εk c†k ck + JK∑Sr·(c†σc) + J∑ Sr · Sr’
Kondo Lattice Model
If {JK,J} >> εk (W), then SCES, e.g. HFLiq, NFL, QCPt.
See sketches. What type of systems ? 4f &5f intermetallics.